## Slide 1: Investigation of Gem Materials using 405nm Laser Spectroscopy
Henry Barwood
Troy University
Troy, Alabama

## Slide 2: 405nm laser diode
GaN diode lasers were developed for Blu-Ray players. They are now widely manufactured in power levels ranging up to 500mW.
Inexpensive diode assemblies are now available in the 5-200mW range, both battery powered (laser pointers) and with AC power supplies and collimating lenses that provide either a spot or line focus.

## Slide 3: 5mW 405nm Laser pointer. Inset 150mW Diode

## Slide 4: 405 nm laser spectrum

## Slide 5: Spectrometer/Diode holder for spectroscopy of small sample areas
A simple holder was constructed that focuses the laser beam onto a small aperture that is centered on the focus of the spectrometer collimator (UV-NIR). The resultant fluorescence is fed into the spectrometer via a standard fiber optic cable (also UV-NIR).

## Slide 6: Laser Diode and Collimator Holder

## Slide 7: Spectrometer modification
An Ocean Optics HR2000 spectrometer was modified with the addition of a new grating that increased the wavelength range to 200-1100nm.
The 10 micron slit on the spectrometer was replaced with a 100 micron slit to improve light gathering power.
A UV-IR fiber optic cable and collimator were added that allow the full 200-1100nm wavelength range. While stiff, a 200 micron fiber was selected for maximum light transmission.

## Slide 8: Laser imaging for photomicrography
Spot focusing lasers are adaptable for imaging gems, small crystals, or areas of petrographic slides.
The high visible output of the laser must be blocked with a yellow filter before a useful image may be obtained.
Imaging as a substage light source is dangerous, and only incident illumination should be used

## Slide 9: Imaging of Samples with an Un-collimated Laser Beam
The output of a laser diode operated without the collimating lens can be scanned across a specimen while the camera is in Bulb mode. This allows the collection of a macro image of the specimen. By blocking most of the visible light with a yellow filter, minerals having a response to the 405nm laser emissions may be imaged. Processing of the images can also provide a quantitative measure of the amount of the fluorescent mineral.

## Slide 10
In order to test the laser fluorescence of diamonds, small < 1mm crystals were purchased from a number of sources. No information as to the actual source localities of the diamonds was available; however, they were simply listed as “Congo”. The body colors of the diamonds were mostly yellow to off white.

## Slide 11: Diamonds Fluorescent colors observed in diamonds using 405 nm laser
Green (common)
Yellow ( 5 examples)
Blue (single example)
Red (single example)

## Slide 12: In all subsequent figures, the fluorescent specimen is pasted in the upper right hand corner of the figure

## Slide 13: Blue luminescent diamond spectrum

## Slide 14: Green luminescent diamond spectrum

## Slide 15: Yellow luminescent diamond spectrum

## Slide 16: Red luminescent diamond spectrum

## Slide 17: Gems showing dominant Cr3+ (and Fe3+) response to 405nm laser
Beryl var. Emerald
Chrysoberyl var. Alexandrite
Corundum var. Ruby
Grossularite var. Tsavorite
Kyanite
Spinel
Spodumene var. hiddenite
Topaz

## Slide 18: Emerald spectrum showing Cr3+ and Fe 3+ (?) activation

## Slide 19: Corundum var. Ruby (synthetic) spectrum showing Cr3+ activation

## Slide 20: Chrysoberyl var. Alexandrite spectrum showing Cr3+ activation

## Slide 21: Grossularite var. Tsavorite spectrum showing Cr3+ and Fe3+ (?) activation

## Slide 22: Comparison of 405nm Spectra for Kyanite Color Variations (line colors correspond to blue, green and orange kyanite). Note Differences in Cr3+ Lines

## Slide 23: Spodumene var. Hiddenite spectrum showing Cr3+ and Fe3+ (?) activation. The green response on the spectrum is from the unknown green luminescing inclusions in the spodumene

## Slide 24: Topaz (Brazil) spectrum showing Cr3+ and weak Fe3+ (?) activation

## Slide 25: Gems showing dominant Mn2+ activation
Fluorapatite
Grossularite
Kyanite
Spodumene var. Kunzite
Titanite
Zoisite var. Tanzanite

## Slide 26: Fluorapatite spectrum showing Mn2+ activation

## Slide 27: Grossular (Mexico) spectrum Mn 2+ activation

## Slide 28: Spodumene var. Kunzite spectrum showing Mn2+ activation

## Slide 29: Pink Tanzanite spectrum showing Mn2+ activation

## Slide 30: Gems showing dominant REE activation (Sm3+ and Dy 3+)
Fluorapatite
Scheelite
Titanite

## Slide 31: Fluorapatite spectrum showing REE activation

## Slide 32: Titanite spectrum showing REE activation

## Slide 33: Scheelite (China) spectrum showing REE activation

## Slide 34: Gems with other activators
Amber (organic)
Axinite
Cancrinite
Chalcedony (Uranium)
Opal (Uranium)
Petroleum and shell (organic)
Scapolite
Sodalite

## Slide 35: Amber (Arkansas) spectrum

## Slide 36: Opal (Hyalite) spectrum showing Uranium activation

## Slide 37: Sodalite spectrum

## Slide 38: Summary of Initial Research
Diamond provenance, and activators need to be defined
Other gem materials should be investigated for additional activators
Potential for gem identification should be investigated