## Slide 1: SPATIAL CORRELATION OF INFRARED AND PL OPTICAL CENTERS IN HYDROGEN-RICH DIAMONDS
Troy Ardon and Sally Eaton-Magaña
Gemological Institute of America
Carlsbad, CA USA

## Slide 2: Geology of Marange
Samples sourced from Marange
Alluvial deposit
Unusually high amount of radiation damage
Commonly found containing hydrogen clouds
Image by Wuyi Wang
Notes: The diamonds we sourced were from the Marange deposit in Zimbabwe…
And of interest to us they … *H clouds*

## Slide 3: Hydrogen Clouds
Granular clouds of unknown structure and composition
Usually highly symmetric
Associated with infrared defect at 3107 cm-1
Image by Jian Xin Liao
Notes: Associated with infrared defect at 3107 cm-1
Which we’ll be returning to

## Slide 4: Experimental Design
Flat plate with uniform thickness
Inscribed a series of points forming axes for accurate and reproducible mapping
Cloud shape thought to show strong contrast in features

## Slide 5: Experimental Design
Infrared (IR) maps taken with Nicolet iN10 IR microscope on a grid with spacing of 100 μm and with an aperture size of 100 μm X 100 μm
Photoluminescence (PL) spectroscopy taken with Renishaw inVia Raman Microscope with 488 nm, 514 nm, and 830 nm lasers on a grid with 500 μm spacing
Heated in a muffler tube furnace to temperatures of 300oC, 600oC, 800oC, 1000oC, and 1200oC for one hour at each step.
After heating to 1200oC, the fractures present developed and the sample broke apart.
Notes: Mention the visible damage in the IR/PL maps

## Slide 6: IR mapping
Main features tracked were the A aggregates, 3123 cm-1 and 3107 cm-1 hydrogen related defect.
There was no detectable signal from B-aggregated nitrogen, indicating the formation temperature was likely below 1100oC[1]
[1] Kiflawi et al., “The creation of the 3107 cm-1 hydrogen absorption peak in synthetic diamond single crystals,” Diamond and Related Materials 5 (1996) pp. 1516-1518

## Slide 7
A aggregates (1280 cm-1)
N3VH (3107 cm-1)
NVH (3123 cm-1)
Wavenumber (cm-1)
1000
5000
4000
3000
2000
0
1
3
2
Absorbance (a.u.)
Infrared Spectrum of IaA type Diamond
Notes: This is a spectrum from a hydrogen rich part of the sample

## Slide 8
A Aggregated Nitrogen
C
C
C
C
C
C
C
C
C
C
C
C
N
N
C
C
C = Carbon
N = Nitrogen

## Slide 9
H
C
C
C
C
C
C
C
C
C
C
C
V
N
C
C
3123 cm-1 Defect
C = Carbon
N = Nitrogen
V = Vacancy
H = Hydrogen

## Slide 10
H
C
C
C
C
C
C
C
N
C
C
C
V
N
C
N
3107 cm-1 Defect
C = Carbon
N = Nitrogen
V = Vacancy
H = Hydrogen

## Slide 11: Temperature Variance of IR Defects
A Nitrogen (1280 cm-1)
3107 cm-1 Defect
Natural
After 1000oC
0.0
1.0
2.0
Absorbance (a.u.)
Notes: Talk about edge scattering effects

## Slide 12: Proposed Mechanisms for Formation of N3VH
N
V
H
N
N
N
N
V
H
N
N
H
+
+
+
V
N
N
V
N
N
N
H
?
?
?

## Slide 13: PL mapping
Tracked peaks of known structure, H3 (503.2 nm), NV- (637.5 nm), H2 (986.2 nm)
Tracked peaks of unknown structure at 523.5, 612.4, 700.5, 926, and 948 nm
Most defects correlated with hydrogen rich areas
Largest increase in defect concentration between 600oC and 800oC (temperature range when vacancies become mobile)

## Slide 14
C
C
C
C
C
C
C
C
N
C
C
C
V
N
C
N
N3 Defect
C = Carbon
N = Nitrogen
V = Vacancy
Not observed in either H-rich or H-poor areas, therefore not a contributor to N3VH

## Slide 15: Proposed Mechanisms for Formation of N3VH
N
V
H
N
N
N
N
V
H
N
N
H
+
+
+
V
N
N
V
N
N
N
H
?
?
?

## Slide 16
C
C
C
C
C
C
C
C
C
C
C
C
V
N
C
N
H3 Defect
C = Carbon
N = Nitrogen
V = Vacancy
Notes: Neutral form of defect, the negative H2 was not detected

## Slide 17
H3 Area
Intensity (arb. units)
0.00
1.20
0.60
0
2
4
2
4
X (mm)
Y (mm)
0
2
4
2
4
Y (mm)
0
2
4
2
4
Y (mm)
0
2
4
2
4
Y (mm)
Natural (no heat)
300oC
600oC
1200oC
0
2
4
2
4
X (mm)
0
2
4
2
4
X (mm)
X (mm)
0
2
4
2
4
Y (mm)
1000oC
X (mm)
0
2
4
2
4
Y (mm)
800oC
X (mm)
Notes: Because this defect was elevated in H rich areas rather than in H poor areas, it is unlikely to have contributed to formation of N3VH

## Slide 18: Proposed Mechanisms for Formation of N3VH
N
V
H
N
N
N
N
V
H
N
N
H
+
+
+
V
N
N
V
N
N
N
H
?
?
?

## Slide 19: Analysis of IR Defect Distribution
Analysis was done along the Y coordinate at evenly spaced X coordinates
Confirmed visual analysis that showed an inverse correlation of A aggregated nitrogen with hydrogen clouds

## Slide 20: Variance along the y-axis of defect concentrations
Chart: 
| 500.0 | 1000.0 | 1500.0 | 2000.0 | 2500.0 | 3000.0 | 3500.0 | 4000.0 | 4500.0 | 5000.0
Aaggregates | 96.8 | 90.47 | 137.48 | 142.33 | 147.38 | 156.72 | 139.86 | 107.56 | 102.05 | 95.99
Scaled3107 | 126 | 129.75 | 23.25 | 5.25 | 7.5 | 8.25 | 77.25 | 130.5 | 122.25 | 127.5
Scaled3123 | 82.5 | 112.5 | 90 | 0 | 0 | 0 | 67.5 | 135 | 82.5 | 82.5
Y Position (μm)
Peak Area (Scaled for reference)
Dashed lines show position of H clouds

## Slide 21: Evidence for Formation Mechanism
Other formation pathways unlikely due to absence of defects
Inverse correlation of A nitrogen shows that A nitrogen is likely depleted during formation of N3VH
Formation pathways involving three or more defects combining likely energetically unfavorable

## Slide 22: NV- Centers
Only defect noted to be elevated in H poor areas
The neutral counterpart (NV0) was not detected
Wavelength (nm)
Intensity (counts)
NV- 637 nm
Diamond Raman Peak 552 nm
NV0 575 nm (Absent)
PL Spectrum of Hydrogen Poor Area (taken with 514 nm laser)
Liquid Nitrogen Artifact

## Slide 23
NV- Centers
Intensity (arb. units)
0.00
2.00
1.00
0
2
4
2
4
Y (mm)
0
2
4
2
4
Y (mm)
2
4
0
2
4
Y (mm)
0
2
4
2
4
Y (mm)
0
2
4
2
4
Y (mm)
0
2
4
2
4
Y (mm)
Natural (no heat)
300oC
600oC
800oC
1000oC
1200oC
X (mm)
X (mm)
X (mm)
X (mm)
X (mm)
X (mm)

## Slide 24: Conclusions and Future Investigations
A-type nitrogen combining with NVH likely formation pathway for N3VH
Many defects of unknown structure correlated with hydrogen-rich areas
Use samples with minimal fractures to push to higher temperatures

## Slide 25: Questions ?