## Slide 1
THE Characterization of Abandoned Mines in New Mexico
John Asafo-Akowuah1, Virginia T. McLemore2 & Ashlynne Winton1
1Department of Mineral Engineering, New Mexico Tech, Socorro, NM 87801
2New Mexico Bureau of Geology and Mineral Resources (NMBGMR), New Mexico Tech, Socorro, NM 87801
GSA ANNUAL MEETING - 2016
09/25/2016

## Slide 2
ACKNOWLEDGEMENTS
Funding Sources
  NMBGMR
  NEW MEXICO TECH
  NM Geological Society
  NEW MEXICO EPSCoR (funded by the National Science Foundation (NSF) award #IIA-1301346)
Appreciation
  Navid Mojtabai
  Ingar Walder
  Lynn Heizler
  Tiffany Lutherback

## Slide 3
OUTLINE
Background
Study Area
Problem Identification
Objectives
Methodology
Observations
Conclusions

## Slide 4
BACKGROUND
1948 – 2002, >347 million pounds of U was produced in NM cumulatively amounting >$ 4.7billion
After effects of Mining & Exploration in NM has resulted in about 300 legacy mines
>1000 uranium occurrences in NM (>100 ppm U, U minerals)
These mines typically include two or more actual mine features
Most of these legacy mines pose little or no environmental or stability threat to the public and environment
New Mexico Mining and Minerals Division (NMMD) has assessed approximately 57 AUM (Abandoned Uranium Mine)

## Slide 5
Loading bin, Lucky Don
Waste pile
Examples of Legacy mine features
Mine face

## Slide 6
STUDY AREA
Lucky Don & Little Davie legacy uranium mines
  Rio Grande Rift Cu-Ag (U) vein deposit type, Permian San Andres Formation
  Lucky Don: 1955–1963 U, V mined from limestone by surface & underground method
  Little Davie: U, V mined from limestone by surface & underground method in 1955
  Estimated value of U produced by Lucky Don & Little Davie $70,000

## Slide 7
STUDY AREA
Jeter legacy uranium mine
  Rio Grande Rift Cu-Ag (U) vein deposit type, fault between Proterozoic Capirote granite and the Miocene (?) sediments
  1954–1958 U, V were mined from disseminated U minerals in the clay zone in fault gouge along the Jeter fault by surface & underground mining methods
  Total U produced from Jeter mine amounts to 58,562 pounds worth ~$500,000

## Slide 8
MAP OF STUDY AREA
Fig1. Mining districts within Socorro County
Fig2. Lucky Don & Little Davie AUM
Socorro

## Slide 9
MAP OF STUDY AREA
Fig3. Jeter AUM

## Slide 10
PROBLEM IDENTIFICATION
Reclamation efforts have not examined the long-term chemical effects from these mines
There is still potential for environmental effects long after remediation of the physical hazards, as found in several areas in NM including Jackpile mine, Laguna
Some of these observations only come from detailed electron microprobe studies
Many more legacy mines in NM, which either have not been safely remediated or closed or their status is unknown

## Slide 11: OUR APPROACH
Data gathering following Bureau of Land Management (BLM) inventory procedure with modifications
Hazard ranking of mine openings and features, using BLM ranking methodology with modifications
Sampling of waste and rock piles
General stability analyses of structures
Determination of criteria for use of existing rock piles for backfill material, location of additional sources of backfill material if available, and estimates of how local weather would affect the remediation

## Slide 12
Laboratory analyses
Paste pH
Geochemistry and mineralogy of samples
  Petrography
  Electron microprobe
  XRF
  XRD
Acid-base accounting

## Slide 13
    To develop a relatively quick and inexpensive procedure to inventory and characterize legacy mines in NM using Lucky Don, Little Davie and Jeter mines all in Socorro county as a case study and applying to other sites in NM
OBJECTIVES

## Slide 14: METHODOLOGY
Waste & rock pile sampling
Water sampling
GPS/ scintillometer map

## Slide 15: OBSERVATIONS (Scintillometer Readings)
Scintillometer readings from Adits and/ or mine face.
Abandoned Uranium Mine | Background Radiation (cps) | Min Radiation (cps) | Max Radiation (cps)
Lucky Don | 20-50 | 100 | 4,435
Little Davie | 20-50 | 120 | 771
Jeter | 10-30 | 80 | 2,000
Radiation reading of 4,435 cps recorded in an adit at Lucky Don

## Slide 16: OBSERVATIONS (Field observation of mine features)
Abandoned Uranium Mine | Mine Feature | Depth of Workings (ft) | BLM Hazard Ranking
Lucky Don | 6 stub adits, loading bin, waste/ rock pile | 0–40 | 1
Little Davie | Pit, short adit, waste/ rock pile | 5–10 | 1
Jeter | Concrete platform, 3 waste pile | 300 | 1
Hazard ranking on a scale of 0 – 4

## Slide 17: OBSERVATIONS (Ore minerals & Paste pH)
Abandoned Uranium Mine | Ore Minerals | Paste pH | Field evidence of potential acid drainage
Lucky Don | tyuyamunite, carnotite, uraninite, Cu minerals, uranophane | ~8.18 | No
Little Davie | tyuyamunite, carnotite, uraninite, Cu minerals, uranophane | ~7.39 | No
Jeter | carnotite, tyuyamunite alunite, pitchblende, malachite, Fe-Mn oxides, clay, azuritite, barite, calcite | ~6.72 | No
No evidence of potential acid drainage from field observation

## Slide 18: OBSERVATIONS (Mineralized samples)
Carnotite
U,V
(uraninite ?)
A mineralized sample of host rock from Lucky Don mine ( 4,435 cps)
A mineralized sample of host rock from Little Davie mine (771 cps)
Samples of waste pile rocks with disseminated carnotite from Lucky Don

## Slide 19: OBSERVATIONS (Electron microprobe)
Backscattered electron (BSE) image of marked area
U,V
U,V

## Slide 20: OBSERVATIONS (Electron microprobe)
CaCO3
Fe
Backscattered electron (BSE) image of marked area

## Slide 21: OBSERVATIONS (Electron microprobe)
U,V
U,V
Backscattered electron (BSE) image of marked area

## Slide 22
PRELIMINARY CONCLUSIONS
No evidence of potential acid drainage from field observations
No pyrite observed in Electron microprobe
No acid drainage inference from paste pH measurements
  ~6.72 indicate neutral, 7.39 and 8.18 indicate moderately alkaline
A hazard ranking of 1 on a scale of 0–4 is low
All 3 mine sites are remote

## Slide 23
FUTURE WORK
General stability analyses of structures
Laboratory analyses
  Geochemistry and mineralogy of samples
    Petrography
    XRF
    XRD
Acid-base accounting

## Slide 24
THANK YOU
QUESTIONS