## Slide 1: Mineralogical characterization of talc ore and commercial talc products from the Gouverneur Mining District, New York
*Brittani D. McNamee
University of Idaho
Mickey E. Gunter
University of Idaho
André E. Lalonde
University of Ottawa
Michael C. Rowe
Washington State University

## Slide 2: Why?
platy talc
asbestiform talc
Notes: funky talc picture

## Slide 3
Gouverneur
Arnold Pit
Talcville
Notes: map of talcville and fowler mines

## Slide 4: Overview
Samples
  tailing samples from Arnold Pit and Talcville mines
  products processed by R. T. Vanderbilt Co.
  Museums / Collections
Goals
  Bulk composition acquired with XRF
  Mineral structures identified with powder XRD
  Precise compositional data via WDS and EDS on polished samples in electron microprobe
  Asbestiform vs. Non-asbestiform morphology and alteration of minerals observed in electron microprobe and by PLM
Notes: polished thin sections
polished grain mounts

## Slide 5: Minerals of interest: ideal formulas & SiO2 / MgO ratios
Amphiboles
tremolite Ca2Mg5Si8O22(OH)2 Wt % SiO2 / MgO = 2.4
anthophyllite Mg7Si8O22(OH)2 Wt % SiO2 / MgO = 1.7
Sheet silicates
talc Mg3Si4O10(OH)2 Wt % SiO2 / MgO = 2.0
serpentine Mg3Si2O5(OH)4 Wt % SiO2 / MgO = 1.0
Notes: Fe in anthophyllite

## Slide 6
Arnold Pit
Notes: R1 (AP_mass_amp) rock

## Slide 7
Arnold Pit
XRF Bulk Composition | 
SiO2 | 60.14
TiO2 | 0.01
Al2O3 | 0.67
FeO* | 0.08
MnO | 0.21
MgO | 31.04
CaO | 3.73
Na2O | 0.22
K2O | 0.03
P2O5 | 0.04
Sum | 96.18
LOI (%) | 3.70
Rietveld | 
tremolite | 29%
anthophyllite | 42%
talc | 29%
serpentine | 0%
Notes: R1 (AP_mass_amp) rock

## Slide 8
Arnold Pit
Notes: R1-T6a (AP_mass_amp)

## Slide 9
Arnold Pit
Notes: R1-T6a (AP_mass_amp)

## Slide 10
Arnold Pit
tremolite | 
SiO2 | 59.78
Al2O3 | 0.18
TiO2 | 0.01
FeO | 0.03
MnO | 0.04
MgO | 26.03
CaO | 12.48
Na2O | 0.44
K2O | 0.07
Oxide Totals | 99.72
F | 0.66
Cl | 0.01
talc | 
SiO2 | 59.35
Al2O3 | 0.09
TiO2 | 0.00
FeO | 0.13
MnO | 0.13
MgO | 33.70
CaO | 0.08
Na2O | 0.03
K2O | 0.03
Oxide Totals | 93.81
F | 0.25
Cl | 0.01
anthophyllite | 
SiO2 | 61.79
Al2O3 | 0.13
TiO2 | 0.00
FeO | 0.10
MnO | 0.22
MgO | 36.11
CaO | 0.47
Na2O | 0.15
K2O | 0.00
Oxide Totals | 99.39
F | 0.41
Cl | 0.00
Notes: R1-T6a (AP_mass_amp)

## Slide 11: Nytal-100
Notes: Nytal-100 (GM2-7-longsplinter)

## Slide 12: Nytal-100
XRF Bulk Composition | 
SiO2 | 54.28
TiO2 | 0.03
Al2O3 | 0.78
FeO* | 0.18
MnO | 0.20
MgO | 28.51
CaO | 8.47
Na2O | 0.22
K2O | 0.13
P2O5 | 0.03
Sum | 92.84
LOI (%) | 6.01
Rietveld | 
tremolite | 59%
anthophyllite | 14%
talc | 20%
serpentine | 8%
Notes: Nytal-100 (GM2-7-longsplinter)

## Slide 13: Nytal-100
WDS SiO2 / MgO  1.8
non-asbestiform anthophyllite  1.7
Notes: Nytal-100 (GM2-7-longsplinter)

## Slide 14: Nytal-100
WDS SiO2 / MgO  2.1
asbestiform talc  2.0
Mg2.9Si4.0O10(OH)2
SiO2 | 28.4
Al2O3 | 0.2
TiO2 | 0.0
FeO | 0.4
MnO | 0.1
MgO | 13.6
CaO | 0.2
Na2O | 0.0
K2O | 0.0
Oxide Totals | 43.8
F | 0.1
Cl | 1.0
low Total due to particle size/epoxy
Notes: Nytal-100 (GM2-7-longsplinter-edge)

## Slide 15: Conclusions
Asbestiform talc forms as an alteration of non-asbestiform anthophyllite
Talc and anthophyllite have similar low Fe content
Sample prep important for EDS & WDS agreement

## Slide 16: Thank You
Questions???