## Slide 1: GEOMECHANICAL EFFECTS OF OILFIELD CHEMICALS ON SAND FAILURE IN RESERVOIR ROCKS
Elizabeth O. Wuyep*
Gbenga F. Oluyemi*
Kyari Yates*
Alfred Akisanya**
*Robert Gordon University, Aberdeen
**University of Aberdeen, Aberdeen
GSA 2015 Annual meeting and Exposition
1 – 4 November, Baltimore, Maryland, USA

## Slide 2: Outline
Introduction
Approaches
Results
Conclusion

## Slide 3: Introduction
Sand failure!!!!!
How does this failure happen?
The role of oilfield chemicals.
Current industry’s approach.

## Slide 4: Limitations of the previous works
The Seto et al., 1997:
- Was restricted to static tests;
- Chemicals utilized have different chemistry entirely from the commonly used oilfield chemicals.
The Oluyemi, 2014:
- the study was restricted to the use of scale inhibitor amongst the wider range of chemicals
- no mechanical test was involved;
- did not use XRD to quantify the mineral composition of the rock before and after chemical treatment.

## Slide 5: So what next…..???
Mechanisms of the effects of oilfield chemicals on the geomechanical strength of reservoir rocks.
Mechanical testing, analytical techniques and a wider range of laboratory chemical applications.
Baseline for further study to quantify the effects of these chemicals on sand failure and production.

## Slide 6: Experimental flow chart
Analytical tests
Particle size analysis
Saturation tests
Mechanical test
XRD
SEM
SEM/EDX

## Slide 7: Saturated fluids
Brine filtered using sintered glass filter papers to eliminate extraneous fines.
A stock of 1% betaine, glutaraldehyde and 5% phosphonate scale inhibitor (ATMP) were prepared by diluting 2.50g and 12.50g of the chemicals respectively in 250ml of brine.
Element | Na | K | Ca | Mg | Ba | Sr | Fe | Cl | SO4 | HCO3
Concentration (ppm) | 24870 | 887 | 785 | 136 | 561 | 108 | 3 | 39800 | 35 | 2014

## Slide 8: Static Saturation Test
Cores inside Brine and chemicals
Brine
Betaine
ATMP
Glutaraldehyde

## Slide 9: Static Saturation Test
Cores inside Brine and chemicals
Effluents from Brine and chemicals
Brine
Betaine
ATMP
Glutaraldehyde
Brine effluent

## Slide 10: Static Saturation Test
Cores inside Brine and chemicals
Effluents from Brine and chemicals
Brine
Betaine
ATMP
Glutaraldehyde
Brine effluent
ATMP effluent
Betaine effluent
Glut. effluent

## Slide 11: Mechanical Test (UCT)

## Slide 12: Results
SEM Image – SST before treatment
SEM Image – SST after treatment
EDX Scan- SST before treatment
EDX Scan – SST after treatment
SEM/EDX results for sandstone before and after treatment
Well-sorted, sub-rounded quartz mineral confirmed by EDX scan (c) .
Fine-grained mineral assemblages resulting from altered mineral constituent.
Evidence of altered minerals spread on the surface of the larger unaltered quartz grains.
(a)
(b)
(c)
(d)

## Slide 13: SEM/EDX results for limestone
SEM Image – LST before treatment
SEM Image – LST after treatment
EDX scan - LST before treatment
EDX scan – LST after treatment
(a)
(b)
(c)
(d)
SEM image (a) shows poorly sorted, rhombohedral calcite as confirmed by EDX.
Evidence of grain loosening in image (b) as a result of alteration caused by chemical – formation interaction.
No alteration feature is observed with image (a).

## Slide 14: Elemental composition of the sandstone using EDX
Elements | Untreated Sandstone atomic wt% | Normalized ratio (element/Si) % | SST treated with Corrosion inhibitor atomic wt% | Normalized ratio (element/Si) % | SST treated with Scale inhibitor atomic wt% | Normalized ratio (element/Si) % | SST in Brine | Normalized ratio (element/Si) %
Na | ND | ND | 0.48 | 2.3 | 1.29 | 6.4 | ND | ND
Mg | 0.61 | 2.5 | 0.23 | 1.4 | 0.49 | 2.4 | nd | ND
Al | 6.25 | 0.3 | 2.92 | 17.6 | 2.81 | 14 | 1.57 | 5.2
Ag | ND | ND | ND | ND | 1.33 | 6.6 | ND | ND
P | 0.25 | 1 | ND | ND | 2.03 | 10.1 | ND | ND
Cl | 1.55 | 6.4 | 0.33 | 2 | 2.07 | 10 | 0.21 | 0.7
K | 0.88 | 3.6 | 1.05 | 6.3 | 0.24 | 1.2 | 0.24 | 0.8
Ca | 0.13 | 0.5 | 4.53 | 27 | 0.10 | 0.5 | ND | ND
Fe | 0.86 | 3.5 | 0.42 | 2.5 | 1.46 | 7.2 | 0.10 | 03
Ti | ND | ND | 0.26 | 1.6 | ND | ND | ND | ND
Si | 24.27 | 100 | 16.56 | 100 | 20.18 | 100 | 30.03 | 100
ND =Not detected

## Slide 15: Elemental composition of the limestone using EDX
Elements | Untreated limestone atomic wt% | Normalized ratio (element/Ca) % | LST treated with Biocide atomic wt% | Normalized ratio (element/Ca) % | LST treated with Corrosion inhibitor atomic wt% | Normalized ratio (element/Cl) % | LST treated with Scale inhibitor atomic wt% | Normalized ratio (element/Ca) %
Na | ND | ND | ND | ND | 33.46 | 93.4 | ND | ND
Mg | 0.26 | 1.5 | 0.32 | 1.3 | 0.58 | 1.6 | 0.37 | 1.3
Al | 0.13 | 0.75 | 0.45 | 1.9 | 1.02 | 2.8 | 2.02 | 6.9
Si | 0.48 | 2.8 | 0.35 | 1.4 | 3.98 | 11.1 | 0.34 | 1.2
S | 0.10 | 0.58 | ND | ND | ND | ND | ND | ND
Cl | ND | ND | 0.15 | 0.6 | 35.84 | 100 | ND | ND
Fe | 0.20 | 1.2 | 0.17 | 0.7 | 0.36 | 1 | 0.24 | 0.8
Ca | 17.29 | 100 | 24.16 | 100 | 3.09 | 8.6 | 29.36 | 100
ND = Not detected

## Slide 16: XRD Analysis before chemical treatment
Quartz (SiO2): 85%
SST_XRD
Calcite = 85%
Quartz = 9%

## Slide 17: XRD Analysis before chemical treatment
Quartz (SiO2): 85%
SST_XRD
Calcite = 85%
Quartz = 9%

## Slide 18: Mechanical Test – Failure effects chemically treated sandstone
Samples | Test rate (mm/min) | Max. Load (N) | Strain (mm/mm) | Stress (MPa) | Young’s modulus (MPa)
Sandstone before treatment | 0.5 | 45,307 | 0.04 | 40.44 | 2,221
Sandstone after treatment | 0.5 | 54,618 | 0.07 | 18.09 | 282

## Slide 19: Mechanical Test- Failure effects of chemically treated Limestone

## Slide 20: Mechanical Test- Failure effects of chemically treated Limestone

## Slide 21: Mechanical Test- Failure effects of chemically treated Limestone
Samples | Test rate (mm/min) | Max. Load (N) | Strain (mm/mm) | Stress (MPa) | Young’s modulus (MPa)
Limestone before treatment | 0.5 | 85,176 | 0.04 | 74.27 | 2,134
Limene after treatment | 0.5 | 78,922 | 0.02 | 45.46 | 2,083

## Slide 22: Particle size distributions test
Substantial Particles introduced into the chemicals
Chemical interaction with core materials
Weakening of the cores grain fabrics
Disintegration of the existed grain–to–grain binding
Release and migration of sand grain.

## Slide 23: Conclusion
Results clearly suggest that oilfield chemicals application:
Altered the grain fabrics of the reservoir rock.
Weakened the UCS.
Caused fine-grained mineral ass.
Future works.

## Slide 24: References
Oluyemi, G.F., 2014. Conceptual Physicochemical Models for Scale Inhibitor-Formation Rock Interaction. Petroleum Science and Technology, 32:3, pp 253 -260.
Seto, M., Engebretson, R.R., VonWandruszka, R., Nag, D.K., Vutukuri, V.S., and Katsuyama, K, (1997). Effect of chemical additives on the strength of sandstone. Int. J. Rock Mech. Min. Sci. Geomech. 34:691.

## Slide 25
Thank you
Questions??