## Slide 1
Fungi-Induced Chemical Weathering of Asbestiform Chrysotile
Alexandré J. Fowler
Cara Santelli
Henry Teng

## Slide 2
Chrysotile
Mg3(Si2O5)(OH)4
NMNH 91261
Introduction | References: 11th Edition Report on Carcinogens | Slide 2 of 18
Chrysotile weathering as CO2 sequestration method via mineral carbonation.
    Park & Fan, 2004
Chrysotile weathering and asbestos remediation by microbes?
  Dissolution of Mg and Si by fungus: Verticillium leptobactrum
    Daghino et al., 2009
  Conversion of chrysotile asbestos to non-fibrous amorphous material by lichens.
    Favero-Longo et al., 2005

## Slide 3
Talaromyces sp.
Introduction | References: Frisvad, 2015 & Encyclopedia of Life | Slide 3 of 18
Isolated from serpentinite soils in Donghai, China
  Henry Teng
  Li et al., 2015

## Slide 4
Iron as a Micronutrient
Introduction | References: 11th Edition Report on Carcinogens Fungal Physiology – David H. Griffin | Slide 4 of 18
Chrysotile: Mg3(Si2O5)(OH)4
Potential trace impurities in chrysotile:
Iron
Aluminum
Nickel
Calcium
Chromium
Manganese
Sodium
Potassium
EDS Spectrum NMNH 91261

## Slide 5
Objectives
Objectives |  | Slide 5 of 18
  (1) Compare the biological weathering effect of Talaromyces sp. on chrysotile when bioavailable iron is present or absent in the culture medium
(2) Compare the effect of pH on the in vitro dissolution of chrysotile under biological and abiotic conditions
(3) Determine if biological weathering by Talaromyces sp. is capable of breaking down the structure of chrysotile in vitro

## Slide 6
Methods | References: Daghino et al., 2009 & Li et al., 2015 | Slide 6 of 18
Experimental Setup
Czapek Media: NaNO3 + KCl + K2HPO4 + MgSO4 + Glucose + 100 ml/L MES buffer
with or without 0.01 g/L FeSO4
Iron (II)

## Slide 7
Iron vs. Iron-Free
Results – Objective 1 |  | Slide 7 of 18
Day 1
Day 3
Day 18

## Slide 8
Silica Problems
Results | Flame AA Analysis & SEM | Slide 8 of 18
Experiment
Controls

## Slide 9
Silica Problems
Results | SEM | Slide 9 of 18
Beam Damage After 2 Minutes of Scanning
Silica Precipitates?

## Slide 10
Iron vs. Iron-Free
Results – Objective 1 | Flame AA Analysis Reference: Daghino et al., 2009 | Slide 10 of 18
Chrysotile: Mg3(Si2O5)(OH)4

## Slide 11
Iron vs. Iron-Free
Results – Objective 1 | X-ray Diffraction Analysis | Slide 11 of 18

## Slide 12
Bio vs. Abiotic
Results – Objective 2 | Flame AA Analysis | Slide 12 of 18
Chrysotile: Mg3(Si2O5)(OH)4

## Slide 13
Bio vs. Abiotic
Results – Objective 2 | X-ray Diffraction Analysis | Slide 13 of 18

## Slide 14
Structural Change?
Results – Objective 3 | X-ray Diffraction Analysis | Slide 14 of 18

## Slide 15
Structural Change?
Results – Objective 3 | SEM | Slide 15 of 18
Abiotic Chemical Weathering
Iron Media
Iron-Free Media
Before Experiment
Controls After Experiment
Biological Weathering
Iron Media
Iron-Free Media
Hyphae
Precipitates
Precipitates

## Slide 16
Conclusions
Conclusions |  | Slide 16 of 18
  (1) Talaromyces sp. has the same biological weathering effect on chrysotile regardless of the presence or absence of bioavailable iron in the culture medium.
(2) pH has the same effect on the in vitro dissolution of chrysotile under both biological and abiotic conditions.
  pH is the controlling factor in biological weathering by Talaromyces sp.
(3) Biological weathering of chrysotile by Talaromyces sp. causes dissolution, but does not break down the structure of chrysotile.

## Slide 17
Future Work
Future Work |  | Slide 17 of 18
  (1) How does mineral structure affect the weathering results?
      -Lizardite
      -Antigorite
(2) How do different species or communities affect chrysotile and other mineral weathering in serpentine soils?
    -Species-specific
    -Metabolite-specific

## Slide 18
Thank You!
Department of Mineral Sciences
Funded Jointly by:
Coauthor: Cara Santelli
Coauthor: Henry Teng
Important References:
Daghino, S. et al., 2009, Weathering of chrysotile asbestos by the serpentine rock-inhabiting fungus Verticillium leptobactrum: FEMS Microbiology Ecology, v. 69 no. 1, p. 132–141.
Favero-Longo, S.E. et al., 2005, Chrysotile asbestos is progressively converted into a non-fibrous amorphous material by the chelating action of lichen metabolites: Journal of Environmental Monitoring, no. 7, p. 764–766.
Li, Z., Xu, J., Teng, H.H. et al., 2015, Bioleaching of Lizardite by Magnesium- and Nickel-Resistant Fungal Isolate from Serpentinite Soils–Implication for Carbon Capture and Storage: Geomicrobiology Journal, v. 32, no. 2, p. 181–192.
Park, A.H.A, and Fan, L.S., 2004, CO2 mineral sequestration: physically activated dissolution of serpentine and pH swing process: Chemical Engineering Science, no. 59, p. 5241–5247.
Special Thanks to: