## Slide 1
Geological Survey of Canada Scientific Presentation Geoenvironmental characterization of mine wastes from carbonatite-hosted niobium deposits: ferroniobium slag A.J Desbarats and J.B. Percival 2019

## Slide 2: Carbonatites
Plug-shaped intrusions consisting of > 50% carbonate minerals (calcite, dolomite, ankerite)
Enriched in incompatible elements (REE, U, Th, Nb, Ta, Zr)
Attractive exploration targets for REE and Nb
Little published information on the environmental signature of mining carbonatites for REE or Nb

## Slide 3: Case study St-Lawrence Columbium mine, Oka, Quebec
Archetypal carbonatite-hosted Nb deposit mined between 1961 and 1976
Different types of mine wastes and mine waters: pit lakes, waste rock, tailings, ferroniobium slag
Focus here on ferroniobium slag: its mineralogy, (radio)chemistry, and leachate chemistry
What are issues of potential environmental concern associated with the slag?

## Slide 4: Simplified geology of the Oka carbonatite complex (from Lentz, 2006)

## Slide 5: Airborne radiometric survey of the study area: equivalent thorium

## Slide 6: Pyrochlore : Nb ore mineral
Formula: A2-xB2O6(OH,F)
A: Na, Ca, Mn, Sr, U, Th, REE
B: Nb, Ta, Ti, Al, Fe, Zr
Oka example (Petruk & Owens, 1975):
Na.15Ca.48Sr.01Mn.01Fe.16U.38Ce.08Nd.01La.02Nb1.66 Ta.05Ti.27Zr.01O6 (OH,F)

## Slide 7: Ferroniobium (FeNb) production via aluminothermic reduction of pyrochlore concentrate
Pyrochlore concentrate (> 50% Nb2O5) contains pyrochlore ± apatite, mica, sulphide minerals
Reaction:
concentrate + Fe2O3 + Al + NaClO3 + CaF2 + CaO = FeNb + slag
FeNb is quite pure
Slag contains all the U and Th (and everything else)

## Slide 8: Slag melt button

## Slide 9: Slag Mineralogy
Hib: hibonite calcium zirconate (not shown)
Prv: REE-Al-Ca-Ti-perovskite Mg-K-beta alumina
Ca-Al-glass

## Slide 10: Slag Mineralogy

## Slide 11: Radiometric survey of the slag disposal area

## Slide 12: Longitudinal radiometric profile of slag disposal area

## Slide 13: Longitudinal radiometric profile of slag disposal area

## Slide 14: Field-scale slag leach experiment

## Slide 15: Evolution of leachate chemistry: conductivity Na-HCO3 type water

## Slide 16: Evolution of leachate chemistry: pH

## Slide 17: Evolution of leachate chemistry: F

## Slide 18: Evolution of leachate chemistry: Al

## Slide 19: Evolution of leachate chemistry: U

## Slide 20: Controls on leachate chemistry: F

## Slide 21: Controls on leachate chemistry: Al

## Slide 22: Controls on leachate chemistry: U speciation

## Slide 23: Conclusions
Ferroniobium slag contains U (mean 1069 ppm) and Th (mean 1574 ppm) with total average specific activity of ≈ 300 Bq/g
45 year old slag exhibits significant chemical and physical weathering
Slag is composed mainly of hibonite, perovskite, and glass
Glass and perovskite phases are the most unstable under oxidizing, near surface conditions

## Slide 24: Conclusions
Slag leachate is alkaline (pH 9) and contains very high concentrations of Al (2.5-8.5 mg/L), F (18-46 mg/L), and moderate levels of U (15-65 µg/L)
Ferroniobium slag is a Technologically Enhanced Naturally Occurring Radioactive Material (TENORM) requiring environmental management

## Slide 25
http://niobec.com/2014/11/20-ans-transformation-niobec/.
Questions?